# Questions Young’s Modulus

- The wire in the diagram is clamped under tension within its elastic limit:

Calculate

- the applied force if the stress within the wire is 2.56 x 106 Pa

- the tension in the wire.

- An aluminium wire of length 0.35m and radius 0.20mm is stretched by 1.4mm.

Young’s modulus of aluminium is 7.0 x 1010Pa.

- Find the strain in the wire.

- Find the stress in the wire.

- Find the cross sectional area of the wire.

- Find the tension in the wire.

  - A wire 2.0m long is loaded until it stretches 2.4cm.

  - Calculate the strain in the wire.

  - The wire originally was measured to have a diameter if 0.3mm. Calculate its cross sectional area.

  - The load applied to produce this extension was 10.4N. Calculate the stress in the wire.

  - Calculate a value for Young’s modulus for this wire.

  - Is the  value calculated in (d) to be considered a reliable value? Why/Why not?

  - An experienced physicist suggests that the value for the cross sectional area measured in (b) may not be quite accurate when the wire is loaded. Explain his reasoning.

# Text boxes

Wire

Cross sectional area = 3.0 x 10-6m2

Tension